# Gemshorn Build Methods

Generated: 2026-05-06

## Build Method Matrix

| Method | Authenticity | Repeatability | Tooling | Best First Size | Main Risk | Recommended Use |
| --- | --- | --- | --- | --- | --- | --- |
| Natural horn | Highest historical fit | Low, each blank differs | Hand tools, drill press, block fitting tools | GEM-HIST-G4 | Horn volume/curve varies and forces empirical tuning | Make the historically informed reference instrument |
| Slip-cast ceramic | Historically plausible clay lineage, modern process | High after shrinkage data | Master, plaster mold, casting slip, kiln | GEM-SC-C5 | Shrinkage and voicing edge movement | Make the repeatable consort family |
| CNC-routed wood split body | Modern adaptation | Medium to high | CNC router, flip jig, clamps, glue-up, fipple tools | GEM-SC-C5 or GEM-HIST-G4 | Glue seam leaks and routed cavity volume error | Make fast prototypes and serviceable teaching instruments |
| 3D printed body | Modern prototype only | High | SLA/FDM printer, sealant, post-processing | GEM-SC-C5 | Mouth safety, porosity, rough windway | Fit/ergonomics tests before committing molds |
| Carved hardwood solid horn | Modern craft adaptation | Low to medium | Carving, gouges, drills, fipple tools | GEM-HIST-G4 | Internal volume hard to control | One-off art instrument |
| Metal spun/formed shell | Modern experimental | Medium after tooling | Metal forming or fabrication | Alto/tenor only | Condensation, sharp edges, tuning vent noise | Research or sculpture, not first playable build |
| Gourd/calabash or seed pod | Folk-adjacent experiment | Low | Hand tools, sealing, block fitting | Small high register | Cracking and inconsistent volume | Acoustic experiment, not production |
| Resin/composite cast | Modern prototype | High | Silicone mold or printed mold, resin safety controls | GEM-SC-C5 | Mouth-contact safety and off-gassing | Non-mouth-contact display or sealed prototype only |

## Method 1: Natural-Horn Gemshorn

Use authentic-horn-build-plan.md and horn-blank-spec.csv.

- Select several domesticated cow, ox, goat, or sheep horn blanks.

- Clean and stabilize the cavity while keeping the tip closed.

- Fit a removable hardwood or plaster block at the wide end.

- Cut the windway and labium before drilling tone holes.

- Tune the closed note by block/window/vent behavior.

- Drill holes undersize, tune low to high, and record final values in validation.csv.

This method should be labeled “historically informed reconstruction.” Do not claim a museum copy unless the exact source instrument and dimensions are known.

## Method 2: Slip-Cast Ceramic Family

Use mold-and-slip-casting-plan.md, family-spec.csv, and hole-schedule-modern.csv.

- Confirm clay shrinkage with test bars.

- Make the GEM-SC-C5 master first.

- Cast a two-part plaster mold around a sealed master.

- Cast one body, bisque, measure volume, and tune.

- Update the design table before scaling to larger family members.

- Keep the windway, labium, tone-hole interiors, and block seat unglazed.

This is the best production path once shrinkage and tuning corrections are measured.

## Method 3: CNC-Routed Split-Wood Body

Use cad/gemshorn_split_wood_body.scad, drawings/gemshorn-cnc-wood-body.svg, and cnc/wood-body-cnc-plan.md.

- Mill two matching wood halves oversized.

- Route registration-pin holes.

- Route mirrored internal cavity halves with a ball end or round-nose bit.

- Add tone-hole pilot marks and fipple/window layout.

- Dry-fit with dowel pins and test the closed cavity for leaks.

- Glue with a thin, continuous, reversible-enough seam strategy for prototypes.

- Shape exterior, cut the voicing, and tune as a vessel flute.

This path is not historically authentic, but it is valuable because the body can be measured, repaired, and iterated without kiln or horn-blank variability.

## Method 4: Prototype And Research Materials

Use material-options.md before committing to any material outside horn, ceramic, or wood. The material must pass three gates:

- It must be safe around the mouth after finish.

- It must hold a crisp labium edge and stable tone-hole edges.

- It must maintain airtight seams and predictable cavity volume.

## Recommended Build Sequence

- CNC-routed wood GEM-SC-C5 to prove the fipple and Helmholtz schedule quickly.

- Slip-cast ceramic GEM-SC-C5 to validate shrinkage and mold process.

- Natural-horn GEM-HIST-G4 to establish the authentic reference voice.

- Expand the ceramic family from C5 outward after measured corrections exist.

# Assembly Manual

Generated: 2026-05-02

## Safety

- Wear a respirator for clay dust, plaster dust, sanding, and fired ceramic grinding.

- Use wet cleanup for clay and plaster; do not sweep dry dust.

- Keep plaster out of reclaim clay.

- Use eye protection when drilling bisque or fired ceramic.

- Use lead-free, food-safe-compatible glazes if the instrument may contact the mouth.

## Tools

- Casting slip, plaster mold, mold straps, buckets, sieve, scale, timer.

- Calipers, flexible ruler, pin gauges, drill bits, tapered reamers, needle files.

- Chromatic tuner or microphone/spectrum app, thermometer, hygrometer.

- Hardwood for blocks, cork/leather/wax for seals, fine saw, knife, small chisels.

- CNC router, dowel-pin fixture, ball end bits, clamps, and leak-test supplies for the split-wood method.

## Build Method Selection

See build-methods.md before starting.

- Use natural horn when authenticity is the goal.

- Use slip-cast ceramic when repeatability and consort scaling are the goal.

- Use CNC split wood when fast iteration and repairability are the goal.

- Use alternate materials only after coupon tests in material-options.md pass.

## Phase 1: Master And Mold

- Pick a size from family-spec.csv.

- Confirm clay shrinkage with test bars.

- Update gemshorn-design-table.xlsx if shrinkage differs from the default.

- Make and seal the master.

- Build a two-part plaster mold using mold-and-slip-casting-plan.md.

## Phase 2: Cast Body

- Pour slip and record drain time.

- Release at leather hard.

- Clean seams, mark centerline, and confirm wall thickness at the pour opening.

- Drill undersize holes from hole-schedule-modern.csv or hole-schedule-historical.csv.

- Trim the fipple seat and window area conservatively.

- Slow dry to bone dry.

## Phase 3: Bisque And Measure

- Bisque fire.

- Measure length, wide OD, hole diameters, mass, and cavity volume.

- Record all measurements in validation.csv.

- Fit a temporary block and test whether the instrument speaks.

## Phase 4: Voice And Tune

- Make the windway even and low.

- Sharpen and stabilize the labium.

- Tune closed note first.

- Open holes gradually from low to high.

- Use wax to backtrack if a hole goes sharp.

- Record every tuning pass, temperature, and action.

## Phase 5: Finish

- Remove block before glaze unless the block is sacrificial.

- Mask windway, labium, hole interiors, and tuning seats.

- Glaze or burnish exterior.

- Glaze fire.

- Refit block, final tune, and seal mouth-contact surfaces.

## CNC Split-Wood Body Method

- Choose the C5 or G4 prototype from build-methods.md.

- Prepare two straight-grained hardwood halves from cut-list.csv.

- Face the mating surfaces and drill registration-pin holes.

- Route mirrored cavity halves using cnc/wood-body-cnc-plan.md.

- Engrave or mark fipple, tone-hole, and datum references.

- Dry-fit the body with dowels and perform the leak test in validation.csv.

- Glue the body only after the cavity volume and leak test pass.

- Shape the exterior, then cut the fipple/window by hand.

- Drill holes undersize and tune low to high.

- Record final volume, pitch, cents error, and finish notes in validation.csv.

## Maintenance

- Keep removable blocks dry and replaceable.

- Avoid soaking fired ceramic bodies unless the clay/glaze combination is proven.

- Store with a cork or cloth spacer so the labium is protected.

- Keep a small wax kit for tuning during outdoor or temperature-variable use.

# Gemshorn Material Options

Generated: 2026-05-06

## Material Selection Rules

A gemshorn body is a closed vessel flute. The material mostly affects durability, edge stability, moisture behavior, weight, and finish, while pitch is dominated by chamber volume, window/vent area, tone-hole conductance, and fipple behavior.

Use any alternate material only after a small coupon proves:

- The labium edge can stay crisp.

- The windway can stay smooth and airtight.

- The material is safe for mouth contact after finish.

- The body can be cleaned and dried without swelling, softening, or shedding dust.

## Candidate Materials

| Material | Build Path | Pros | Risks | Recommendation |
| --- | --- | --- | --- | --- |
| Cow/ox/goat/sheep horn | Natural horn | Strong authenticity, beautiful surface, naturally curved closed cone | Variable volume, odor/dust while working, ethical sourcing | Best authentic reference path |
| White stoneware casting slip | Slip-cast | Durable, repeatable, historically plausible clay form | Shrinkage, warping, glaze shifts pitch | Best production family path |
| Porcelain casting slip | Slip-cast | Fine detail, crisp holes, clean white body | More brittle, shrinkage can be high | Good after stoneware pilot |
| Maple, cherry, pear, boxwood | CNC split wood | Stable, machinable, good edge detail | Glue seam leaks, humidity movement | Best CNC router path |
| Cedar or cypress | CNC split wood/block | Easy to work, light, traditional windway/block feel | Soft labium, dents, resin/finish concerns | Good for removable blocks, not first body |
| Bamboo or cane | Hand-built tube/horn-like adaptation | Light, musical, low cost | Natural tube is not horn-shaped and tip sealing is awkward | Good experiment, not authentic gemshorn |
| Gourd/calabash | Hand-built vessel | Folk resonance, light | Cracks, inconsistent wall, hard fipple seat | Experimental only |
| SLA resin | Printed prototype | Accurate shape, fast iteration | Mouth safety and post-cure uncertainty | Use for masters or non-mouth-contact prototypes |
| PETG/PLA | FDM prototype/master | Cheap, fast, good mold master after sealing | Layer leaks, rough windway, heat sensitivity | Use as mold master, not final instrument |
| Machinable wax/tooling board | CNC master | Stable for mold masters | Not final instrument material | Excellent for plaster mold masters |
| Aluminum/brass/copper | Metal shell | Durable, striking look | Condensation, thermal feel, sharp-edge risk, fabrication complexity | Advanced research only |
| Acrylic/polycarbonate | CNC/laser/formed prototype | Transparent tuning demo | Mouth safety, solvent crazing, brittle chips | Teaching display only unless safety proven |
| Bone/antler | Hand-built | Dense and visually related to horn | Ethical sourcing, dust hazards, small sizes | Avoid for first builds |

## Preferred Material Stack

| Component | Preferred | Acceptable Substitute | Avoid |
| --- | --- | --- | --- |
| Authentic body | Domesticated horn | Burnished ceramic historical pilot | Wild/endangered horn |
| Ceramic production body | White stoneware slip | Porcelain slip | Unknown shrinkage hobby clay |
| CNC wood body | Maple, cherry, pear, boxwood | Walnut, birch, beech | Open-pore oily woods near mouth |
| Fipple/block | Pear, maple, cedar | Plaster or sealed hardwood | Soft crumbly wood, toxic finishes |
| Gasket/seal | Cork, leather, beeswax | Food-safe silicone | Permanent brittle epoxy at tuning joints |
| Finish near mouth | Burnish, shellac after safety review, food-safe oil/wax | Exterior-only glaze away from windway | Heavy glaze in windway or hole interiors |

## Material Experiments Worth Doing

- Ceramic body with wood removable block.

- CNC maple split body with cork gasket and reversible block.

- Transparent acrylic section model for teaching airflow and cavity behavior.

- 3D printed master versus CNC tooling-board master shrinkage comparison.

- Porcelain versus stoneware tuning shift after glaze fire.

# Risks

Generated: 2026-05-06

## Acoustic

### Acoustic: Helmholtz model overpredicts playable pitch

Symptom: The closed note or upper scale speaks flat/sharp even when the calculated cavity volume and tone-hole areas match the design sheet.

Mechanism: Gemshorn pitch depends on coupled fipple/window behavior, leakage, tone-hole chamfer, and effective neck length. The first-pass Helmholtz model is directionally useful but not a finished calibration.

Test: Build GEM-SC-C5 first, measure fired water-fill volume, record the closed note and each opened-hole note at logged temperature, and compute cents error in validation.csv.

Mitigation: Update the design table with measured volume and empirical hole corrections before scaling to the full family. Keep holes flat/undersized before final tuning.

Severity: Medium.

### Acoustic: CNC wood seam leakage weakens fundamental

Symptom: The CNC-routed wood version sounds airy, unstable, or low in volume compared with ceramic/horn.

Mechanism: Split-blank construction creates a long glue seam around the cavity. Even tiny leaks reduce acoustic conductance control and can change the fipple response.

Test: Before final shaping, plug the window and tone holes, gently pressurize the cavity by mouth or bulb, and brush soapy water along the seam.

Mitigation: Add a continuous shallow gasket groove, use a thin even glue line, and seal the interior before final glue-up if the finish is mouth-safe after cure.

Severity: Medium.

## Structural

### Structural: Ceramic cracks around large low-register holes

Symptom: Bass/tenor bodies crack during drying, bisque, drilling, or tuning around H6/T1 or the tuning vent.

Mechanism: Large holes interrupt a curved ceramic shell and create stress concentration. Wall thickness and drying gradients matter more on the larger family members.

Test: Make a clay coupon with the largest bass hole and wall target. Dry and bisque it before committing to the full bass mold.

Mitigation: Add local boss thickness around large holes, drill greenware undersize, slow dry under loose cover, and tune after bisque with gradual reaming.

Severity: High. Human decision required before cutting a bass mold if coupon fails.

### Structural: Natural horn delaminates or cracks during cleaning

Symptom: A horn blank flakes, splits, or opens at the tip while being cleaned or drilled.

Mechanism: Horn is layered keratin. Heat, aggressive soaking, old dry material, or internal defects can delaminate the blank.

Test: Inspect with light through the wall, flex gently at the wide end, and clean one sacrificial blank before layout.

Mitigation: Buy multiple blanks, avoid boiling unless tested, keep the tip closed or permanently plug it, and reject thin/transparent wall sections near the voicing.

Severity: Medium.

## Ergonomic

### Ergonomic: Bass F body exceeds comfortable hand support

Symptom: The bass F is hard to hold, requires wrist extension, or pulls the mouthpiece angle downward.

Mechanism: The scaled bass body is long and wide enough that the instrument behaves like a small supported vessel rather than a hand flute.

Test: Make a cardboard or foam full-scale silhouette from family-spec.csv and check seated/lap, sling, and stand support positions.

Mitigation: Treat GEM-SC-F3 as bench/lap/sling-supported, move holes for reach without assuming position strongly determines pitch, and add a support point to the design drawing.

Severity: Medium.

### Ergonomic: Sopranino holes are too small for reliable playing

Symptom: The sopranino F plays inconsistently because fingertips cannot seal tiny holes precisely.

Mechanism: Scaling reduces tone-hole diameters and spacing. Small holes are tuning-sensitive and are easily rounded by finish or reaming.

Test: Make a flat fingerboard coupon with final hole diameters and ask the intended player to cover holes without looking.

Mitigation: Keep the sopranino as an optional family member, use a slightly larger body scale if needed, or omit chromatic ambitions on that size.

Severity: Low.

## Supply

### Supply: Ethical horn blanks are inconsistent

Symptom: Purchased horn blanks differ too much in curve, wall, odor, core condition, or closed-tip geometry.

Mechanism: Natural horn is not an industrial material. Blank descriptions rarely specify internal volume or fipple-friendly wide-end geometry.

Test: Order several candidate blanks and log length, wide OD, wall, tip condition, water volume, and rejection reason in horn-blank-spec.csv notes.

Mitigation: Buy extras, tune each horn as a one-off, and keep the ceramic/CNC paths as repeatable alternatives.

Severity: Medium.

### Supply: Clay shrinkage data is missing or batch-specific

Symptom: Fired parts do not match master dimensions, and the family scale drifts.

Mechanism: Casting slip shrinkage varies by clay body, water content, mold age, drying, firing cone, and glaze schedule.

Test: Fire shrinkage bars with every clay batch and compare green, bone-dry, bisque, and glaze dimensions.

Mitigation: Update gemshorn-design-table.xlsx before master fabrication and keep masters editable until the clay body is locked.

Severity: High. Human decision required before production mold set if shrinkage is unmeasured.

## Fit/Finish

### Fit/Finish: Glaze or finish rounds the labium edge

Symptom: The instrument becomes breathy, slow to speak, or loses pitch stability after finishing.

Mechanism: The labium and windway need crisp, controlled edges. Glaze, oil, wax buildup, or sanding dust can change the edge and windway height.

Test: Photograph and measure the window before and after finish. Test-blow with the same temporary block before and after finishing.

Mitigation: Mask windway, labium, hole interiors, and block seats. Use exterior-only finish near the voicing and retouch the labium after firing/finish only with controlled tools.

Severity: High. Human decision required if the finish system cannot keep the voicing clean.

### Fit/Finish: Wood body glue line is visible or uncomfortable

Symptom: The routed wood body has a visible seam, rough mouth feel, or finish witness line along the body.

Mechanism: Split-body construction exposes a longitudinal seam and can leave mismatched grain or finish absorption.

Test: Make one finish coupon with the planned glue, seal coat, and final finish; inspect under raking light and touch around the mouth area.

Mitigation: Choose straight-grained matched halves, place seam away from lips/fingers where possible, scrape flush before finish, and use a mouth-safe topcoat.

Severity: Low.

# Validation Report

Generated: 2026-05-06

Verifier command:

python3 /mnt/c/Users/Tony/.codex/skills/instrument-maker-v4/scripts/validate_packet.py . --fix --json

Result: clean. No pass-1 findings and no fixes required.

## Clean Checks

- Tier 1 packet files are present: design, BOM, sourcing, cut list, validation, assembly manual, RFQ, drawing brief, visual BOM brief, Wolfram starter, risks, capstone deck, print packet, manifest, and README.

- Capstone deck has 15 slides, above the v4 verifier threshold.

- README is no longer a minimal scaffold and references an existing hero drawing.

- Referenced drawing files exist.

- print-packet.pdf exists.

- capstone-deck.pptx exists.

- CSVs load successfully.

- SVG drawings parse as XML.

- gemshorn-design-table.xlsx passes zip integrity checks.

## Fixed In v4 Verifier Loop

None. The final verifier pass reported no findings before applying fixes.

## Escalated

None from the packet verifier.

## Remaining Human Measurements

These are not verifier failures; they are shop measurements needed after first prototypes:

- Clay shrinkage by actual slip batch and firing schedule.

- Fired ceramic water-fill volume.

- Natural-horn blank measured volume and final hole diameters.

- CNC wood split-body leak test result.

- Measured Hz and cents error for each prototype.